## IKO Cambridge Architectural Shingles

Specifications & Standards

**STANDARDS**

ASTM D3462

ASTM D3161 Class F

ASTM E108/UL 790 Class A

ASTM D7158 Class H

CSA A123.5 (In Canada)

Miami-Dade Approved³

**SPECIFICATIONS**

Size

1 038 mm x 349 mm (40 7/8" x 13 3/4")

Exposure

149 mm (5 7/8")

Coverage Per Package

3.1 m² (33.3 sq. ft.)

Quantity Per Pallet

56 bundles

Shingles Per Square

60

Quantity Per Unit/Package

20 shingles

Warranty Term

Limited Lifetime¹

Limited Wind Warranty Upgrade

210 km/h / 130 mph¹

Fire Resistance Rating

Class A